TECHNICAL REQUISITION FOR PIPING INSTALLATION

Unit No.: Not Applicable

Unit Abbreviation.: -

Document Class: Z

| Issue Purpose |  |
| --- | --- |

| Rev | Date | Page | Description | Prepared by PTSC | Reviewed by PTSC | Approved by PTSC |
| --- | --- | --- | --- | --- | --- | --- |
| A |  | All | First Issue |  |  |  |

Table of Contents

1.	PURPOSE	3

2.	DEFINITION	3

3.	CODES AND STANDARDS	3

4.	SCOPE OF WORK.	3

4.1	General Scope.	3

4.2	Specific Activities	4

5.	Technical Requirements.	4

5.1	General and Personnel Requirments.	4

5.2	Material Handling and Storage	5

5.3	Technical requirments.	5

5.4	Quality Assurancce and Quatily Control Requirements.	7

5.5	Health, Safety and Environment (HSSE)	8

6.	ATTACHMENT	9

# PURPOSE

Nghi Son Refinery and Petrochemical LLC (NSRP) is plans to replace the Steam Turbine Generator Package 113-A-003 with a new Steam Turbine Generator 113-A-006 on “like-to-like” basis.

This document This document defines the minimum technical requirements for the fabrication, welding, non-destructive examination (NDE), installation, testing, pre-commissioning of piping line.

Name of Owner: Nghi Son Refinery and Petrochemical Limited Liability Company.

Location: NSRP plant, Nghi Son Economic Zone, Hai Yen Commune, Nghi Son District, Thanh Hoa Province, Viet Nam.

# DEFINITION

| ###### PROJECT | ###### STG-3 Replacement Project |
| --- | --- |
| ###### NSRP | ###### Nghi Son Refinery and Petrochemical LLC |
| ###### CONTRACTOR/ PURCHASER | ###### PetroVietnam Technical Services Corporation (PTSC) |
| ###### SUBCONTRACTOR | ###### The supplier of specified services |

# CODES AND STANDARDS

All piping fabrication, installation, inspection, testing, and pre-commissioning activities shall comply with the latest editions of the following codes, standards, and specifications unless otherwise specified in the project documents.

ASME B31.3: Process Piping.

ASME B16.5 – Pipe Flanges and Flanged Fittings

ASME B16.20 – Metallic Gaskets for Pipe Flanges

API 570: Piping Inspection.

ASME Section IX:  Welding, Brazing, and Fusing Qualifications

ASME Section V:  Non-Destructive Examination

Project Procedure, Specifications and Approved Vendor Documents

# SCOPE OF WORK.

  - General Scope.

The implementation of responsibilities shall be in alignment with the EPC Contract between NSRP and PTSC. Regarding the execution of the Works, the Subcontractor shall be entitled to benefits received by PTSC from NSRP and shall be liable to PTSC for the responsibilities that PTSC holds toward NSRP within the scope of piping line.

The Subcontractor shall provide all management, labor, supervision, materials, tools, and equipment required for the fabrication, installation, testing and precommissioning of piping line in accordance with project specifications, drawings, and applicable international standards.

  - Specific Activities

The scope includes, but is not limited to:

- Site Survey and Risk Assessment: Comprehensive site verification and HSE risk evaluation prior to mobilization.

- Procurement and Supply: Supply of required tools, equipment, materials and consumables.

- Welding and NDT: Execution of all welding and Non-Destructive Testing in lieu of previous bonding requirements.

- Field Installation: Rigging, fit-up, alignment, welding and final installation of piping and accessories.

- Surface Protection: Application of coating/painting systems.

- Pressure Testing and internal cleaning.

- Regulatory/Owner Approval:  Obtaining specific approval from NSRP for each individual line completion.

The pipelines designated for piping line installation work are listed in the attachment #1: Isometric drawing and P&ID drawing.

# TECHNICAL REQUIREMENTS.

This section consolidates all general, technical, quality, and safety requirements necessary for the successful execution of the piping works for the STG-3 Replacement Project.

  - General and Personnel Requirments.

- Compliance: All work must be carried out in accordance with approved project drawings, NSRP specifications, and international standards.

- Material Integrity: All pipes, fittings, and accessories must be sourced from approved manufacturers and handled/stored properly to prevent mechanical damage or contamination

- Personnel Qualification:  Welders and NDT Technicians must be qualified per ASME Section IX and Section V respectively. Qualification records must be submitted to PTSC/NSRP for review and approved.

- Pre-execution Submittals: Before starting work, the following must be submitted for approval: Method Statements, Inspection and Test Plans (ITPs), Installation Procedures, and Material Certificates.

- Submittals:  No work shall commence without approved Method Statements, Inspection and Test Plans (ITPs), and Installation Procedures.

  - Material Handling and Storage

- Materials shall be inspected upon receipt (size, rating, material grade, heat number).

- Carbon steel and stainless steel shall be stored separately.

- Stainless steel shall be protected from contamination (no direct contact with carbon steel).

- Pipes shall be stored on wooden sleepers and protected from corrosion and damage

  - Technical requirments.

- Cutting, beveling and preparation.

- Cutting and beveling shall be carried out using approved methods (machine cutting preferred).

- Bevel angle and root face shall comply with approved WPS.

- Fit-up shall ensure proper alignment, root gap, and no excessive mismatch.

- All edges shall be cleaned before welding (free from oil, rust, moisture).

- Welding Requirements.

- Welding shall be performed in accordance with approved WPS/PQR.

- Welders shall be qualified as per ASME Section IX.

- Preheating and PWHT shall be applied when required by specification.

- Electrodes and filler materials shall be properly stored and controlled (oven/drying)

- Subcontractor shall maintain a comprehensive Weld Map and Weld Summary Report for every line. These documents must track welder IDs, date of welding, NDT results, and visual inspection clearance

- Installation Requirements.

- Installation shall follow isometric drawings and piping layout.

- Proper alignment with equipment nozzles shall be ensured (no undue stress).

- Pipe supports shall be installed as per drawings:

- Fixed, guide, and sliding supports as required

- Spring supports shall be preset and locked before installation

- Correct slope shall be maintained for drain and vent lines.

- Flanged Joints Assembly of flanged joints shall be performed in accordance with ASME PCC - 1. Subcontractor must use approved gaskets and follow the documented bolt tightening sequence to ensure uniform load distribution and leak-free performance.

- Inspection and NDT

- Material Inspection:

- Verify materials upon receipt _ Size, thickness, rating, and material grade. Heat number and traceability.

- Check for visual defects: Corrosion, dents, cracks

- Ensure proper identification and segregation (CS vs SS).

- Fit-up Inspection. Verify before welding:

- Alignment and dimensional tolerance

- Root gap and bevel angle as per approved WPS

- Cleanliness of joint (free from oil, rust, moisture)

- Welding Inspection

In-process inspection:

- Preheat temperature (if required)

- Interpass temperature control

- Ensure welding consumables are properly controlled and recorded.

- Visual inspection shall be conducted for all welding joints: Weld profile, reinforcement, undercut, overlap, cracks.

- NDT (RT/UT/MT/PT) shall be performed as per project specification and piping class.

- Pressure testing requirements.

- Pressure testing shall be performed in accordance with ASME B31.3 (for process piping) or applicable project specification, and

- Test pressure:

- Minimum 1.5 × design pressure (unless otherwise specified).

- Test medium:

- Clean water with corrosion inhibitor (if required).

- Test duration:

- Minimum 30 minutes holding time after stabilization.

- Acceptance criteria:

- No visible leakage.

- No pressure drops beyond allowable tolerance.

- All vents shall be opened during filling to remove air pockets.

- Pressure gauges shall be calibrated and installed at appropriate locations.

- Temporary supports/restraints shall be provided where required.

- After testing, system shall be completely drained and dried.

- Pre-commissioning requirements.

The pre-commissioning phase shall ensure that all steel piping systems are clean, dry, and mechanically complete, ready for safe operational startup.

- Internal Cleaning Methods: Appropriate cleaning methods shall be selected based on service requirements, pipe material, and system criticality. The following methods shall be applied as applicable but not limited.

- Water Flushing: All piping systems shall be flushed with clean water to remove welding slag, mill scale, debris, and other foreign materials. Where required, corrosion inhibitors or chemical additives may be introduced to enhance cleaning effectiveness.

- Air Blowing: Dry, oil-free compressed air shall be used to remove loose particles, dust, and residual moisture from piping systems. Air blowing shall be conducted at sufficient velocity to ensure effective cleaning, particularly for instrument air and utility lines.

- Steam Blowing: Steam blowing shall be performed for steam lines and critical service piping to remove internal contaminants such as rust, scale, and construction debris. The procedure shall meet the acceptance criteria (e.g., target plate method) to verify system cleanliness.

- System Reinstatement: Following completion of testing and cleaning, all temporary items such as blinds, spacers, and test gaskets shall be removed. Permanent gaskets and bolting shall be installed in accordance with ASME PCC-1, ensuring proper bolt tightening sequences and torque requirements.

- Support and Equipment Verification: A final inspection shall be carried out to confirm that all pipe supports (fixed, guide, and sliding types) are correctly installed. Spring supports shall be released from temporary locking devices. Alignment between piping and equipment nozzles shall be verified to avoid excessive stress.

- Venting: All high-point vents used during flushing or filling operations shall be properly closed after completion.

- Documentation Requirements.

The Contractor shall submit the following documents:

- Method Statement.

- Inspection and Test Plan (ITP).

- Material certificates.

- Installation reports.

- Test reports.

- As-built drawings.

  - Quality Assurancce and Quatily Control Requirements.

- The Subcontractor shall implement a comprehensive QA/QC program to ensure that all steel piping works comply with project technical specifications, applicable codes, and international standards

- The contractor shall establish a QA/QC program in compliance with ISO 9001-2015 quality management System.

- Personnel Qualification:

- All welders shall be qualified in accordance with ASME Section IX.

- All NDT personnel shall be qualified in accordance with ASME Section V or equivalent recognized standards.

- Qualification records shall be submitted to PTSC and NSRP for review and approval prior to commencement of work.

- Welding Control:

- All welding activities shall be performed in accordance with approved Welding Procedure Specifications (WPS) supported by qualified Procedure Qualification Records (PQR).

- The Subcontractor shall maintain a detailed Weld Map and Weld Summary Report for each piping system, including: Weld identification number, Welder identification, Welding date, Visual inspection status, NDT method and results.

- Inspection and Test Plan (ITPs) - No work shall commence without an approved ITP. The ITP shall define all inspection and test activities, including but not limited to:

- Fit-up Inspection: Verification of joint alignment, bevel configuration, root gap, and cleanliness prior to welding.

- In-process Inspection: Monitoring and recording of preheat temperature, interpass temperature, and welding parameters.

- Non-Destructive Testing (NDT): Execution of required examinations such as Radiographic Testing (RT), Ultrasonic Testing (UT), Magnetic Particle Testing (MT), and Liquid Penetrant Testing (PT), in accordance with applicable piping class and project specifications.

- Pressure Testing Documentation: Hydrostatic pressure tests shall be properly recorded, including calibrated pressure gauge certificates, test pressure, test duration, and stabilization period.

- Final Quality Dossier - Upon completion of the works, the Subcontractor shall submit a comprehensive Quality Dossier, including:

- Material certificates (MTC)

- Welding records (WPS, PQR, WPQ)

- Weld maps and weld summary reports

- NDT reports

- Pressure test reports

- Inspection records

- As-built drawings

  - Health, Safety and Environment (HSSE)

All activities related to steel piping work shall strictly comply with project HSSE requirements. The following mandatory safety measures shall be implemented:

- Site Survey and Risk Assessment: Prior to mobilization, a detailed site survey and verification shall be conducted. A comprehensive HSE risk assessment (JSA) shall be performed to identify potential hazards associated with the STG-3 replacement project and to establish appropriate control and mitigation measures

- Personnel Protection: All personnel shall wear appropriate Personal Protective Equipment (PPE) at all times, including during cutting, grinding, welding, and other construction activities. PPE shall comply with project specifications and relevant safety standards.

- Safe Lifting and Rigging: All lifting and rigging operations, particularly for large-diameter piping, shall be properly planned and executed in accordance with approved lifting plans. Certified lifting equipment and qualified rigging personnel shall be used to prevent injury and equipment damage.

- Hazardous Materials Handling: All hazardous substances, including chemicals used for cleaning, NDT, and touch-up painting, shall be handled, stored, and disposed of in accordance with applicable Safety Data Sheets (SDS) and project specifications.

- Hot Work Safety: All welding, cutting, and grinding activities shall be conducted under an approved Permit to Work (PTW) system. Adequate fire prevention measures shall be implemented, including fire watch personnel, fire extinguishers, and gas testing where required, in compliance with NSRP plant regulations.

- Waste Management and Environmental Protection: The Subcontractor shall maintain good housekeeping at all times. Construction waste shall be properly segregated, handled, and disposed of in accordance with local regulations and project environmental requirements. Measures shall be implemented to prevent environmental contamination.

- Personnel Qualification and Site Access: Only personnel who have completed required HSSE inductions and hold ID cards shall be allowed to enter the site. All personnel shall comply with site safety rules and regulations at all times.

# ATTACHMENT

###### Attachment #1: Isometric drawing and P&ID drawing.

###### Attachment #2: Material specification

###### Attachment #3: STG3 Line list

###### Attachment #4: QA/QC doccuments.