TECHNICAL REQUISITION FOR GRP&GRE PIPE FABRICATION AND INSTALLATION

Unit No.: Not Applicable

Unit Abbreviation.: -

Document Class: Z

| Issue Purpose |  |
| --- | --- |

| Rev | Date | Page | Description | Prepared by PTSC | Reviewed by PTSC | Approved by PTSC |
| --- | --- | --- | --- | --- | --- | --- |
| A |  | All | First Issue |  |  |  |

Table of Contents

1.	PURPOSE	3

2.	DEFINITION	3

3.	CODES AND STANDARDS	3

4.	SCOPE OF WORK.	3

4.1	General Requirements.	5

4.2	Technical requirments.	5

4.3	Quality Assurancce and Quatily Control Requirements.	7

4.4	Health, Safety and Environment (HSSE)	7

5.	ATTACHMENT	7

# PURPOSE

Nghi Son Refinery and Petrochemical LLC (NSRP) is plans to replace the Steam Turbine Generator Package 113-A-003 with a new Steam Turbine Generator 113-A-006 on “like-to-like” basis.

This document outlines the minimum technical requirements, procedures, and safety measures for performing fabrication, testting, cleaning and installaion of GRP / GRE piping line.

Name of Owner: Nghi Son Refinery and Petrochemical Limited Liability Company.

Location: NSRP plant, Nghi Son Economic Zone, Hai Yen Commune, Nghi Son District, Thanh Hoa Province, Viet Nam.

# DEFINITION

| ###### PROJECT | ###### STG-3 Replacement Project |
| --- | --- |
| ###### NSRP | ###### Nghi Son Refinery and Petrochemical LLC |
| ###### CONTRACTOR/ PURCHASER | ###### PetroVietnam Technical Services Corporation (PTSC) |
| ###### SUBCONTRACTOR | ###### The supplier of specified services |

# CODES AND STANDARDS

All works shall comply with the latest editions of the following standards where applicable:

ASME B31.3: Process Piping.

API 570: Piping Inspection.

ISO 14692: GRP piping systems for the oil and gas industry.

ASTM D2996: Filament-wound fiberglass pipe.

ASTM D2563: Visual defects for reinforced plastic laminates.

Project Procedure, Specifications and Approved Vendor Documents

# SCOPE OF WORK.

The implementation of responsibilities shall be in alignment with the EPC Contract between NSRP and PTSC. Regarding the execution of the Works, the Subcontractor shall be entitled to benefits received by PTSC from NSRP and shall be liable to PTSC for the responsibilities that PTSC holds toward NSRP within the scope of GRP&GRE piping line fabrication and installation.

The Sub-contractor shall provide fabrication, supply, and installation services for GRP (Glass Reinforced Plastic) and GRE (Glass Reinforced Epoxy) piping systems in accordance with project specifications, drawings, and applicable international standards.

The scope includes but is not limited to:

- Fabrication of GRP/GRE pipes and fittings.

- Supply of required tools, equipment, materials and consumables.

- Field installation of piping systems.

- Lamination and bonding works.

- Alignment and support installation.

- Hydrostatic testing and inspection.

- Surface protection and finishing (if applicable).

- Documentation and quality records.

The pipelines designated for “GRP & GRE piping line fabrication and installation” work are listed in the table-1 below:

| No. | Line No | Pipe class | Material | Size (in) | Design Pressure (kpag) | Op. Pressure (kpag) | Design Temp (degC) | Op. Temp (degC) | Test Pressure (kpag) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 32”-CSWR-113-4301-S0CW-NI | S0CW | GRP | 32 | 1000 | 150 | 65 | 43 | 1500 |
| 2 | 32”-CSWR-113-4301-S0CW-NI | S0CW | GRP | 32 | 1000 | 150 | 65 | 43 | 1500 |
| 3 | 32”-CSWS-113-3001-S0CW-NI | S0CW | GRP | 32 | 1000 | 150 | 65 | 43 | 1500 |
| 4 | 32”-CSWS-113-4301-S0CW-NI | S0CW | GRP | 32 | 1000 | 150 | 65 | 43 | 1500 |

- Collection of related documents

- Performance of scope in the scope area (refer to the attachment #1: Isometric drawing and P&ID drawing).

- Piping material specification: S-000-1360-0002V (refer to the attachment #2: Material specification).

- Line list for steam turbine generators: S-113-1228-0001S (refer to the attachment #3: STG3 Line list).

###### Conduct site survey and risk assessment.

###### Supply and install required pipe, fittings, valves, and other accessories.

###### Perform mock-up for Lamination & Bonding if required by NSRP.

###### Perform fabrication & installation as per project specifications.

###### Obtain approval from the NSRP for each individual line.

## General Requirements.

The fabrication and installation of GRP and GRE piping systems shall comply with the following general requirements:

- All works shall be carried out in accordance with the approved project drawings, specifications, and applicable international standards.

- The Subcontractor shall ensure that all GRP/GRE pipes, fittings, adhesives, laminating materials, and accessories are supplied by approved manufacturers and are suitable for the specified service conditions.

- Fabrication and installation activities shall be performed strictly in accordance with the pipe manufacturer’s recommended procedures and installation manuals.

- All personnel performing fabrication, lamination, jointing, and installation works shall be properly trained and qualified for GRP/GRE product manuafacture.

- The Contractor shall submit relevant technical documents for approval prior to execution, including but not limited to:

- Method Statement

- Inspection and Test Plan (ITP)

- Installation Procedures

- Material Certificates

- Proper handling, storage, and transportation of GRP/GRE materials shall be ensured to prevent mechanical damage, contamination, or exposure to conditions that may affect material properties.

- All tools and equipment used for fabrication and installation shall be suitable for GRP/GRE piping works and maintained in good working condition.

- Dimensional tolerances, alignment, and installation accuracy shall comply with the project specifications and manufacturer’s requirements.

- Insurance (including professional indemnity insurance) for SUBCONTRACTOR personnel;

- Daily and Weekly Report.

## Technical requirments.

- Fabrication Requirements.

- Fabrication of GRP/GRE pipes and fittings shall be carried out in accordance with approved drawings, project specifications, and manufacturer’s fabrication procedures.

- Pipe cutting shall be performed using suitable tools designed for GRP/GRE materials to ensure clean and square pipe ends without cracking, fiber damage, or delamination.

- Pipe ends shall be properly beveled and prepared prior to jointing as recommended by the manufacturer.

- Bonding surfaces shall be clean, dry, and free from dust, oil, grease, and contaminants before applying adhesives or laminating materials.

- Fabrication of pipe spools and fittings such as elbows, tees, reducers, and flanged connections shall comply with the dimensional tolerances specified in approved shop drawings.

- Adhesives, resins, and reinforcement materials used for bonding and lamination shall be compatible with the pipe material and approved by the pipe manufacturer.

- Fabrication activities shall be performed under controlled environmental conditions within the temperature and humidity limits specified by the manufacturer.

- All personnel performing fabrication, lamination, jointing, and installation works shall be properly trained and qualified for GRP/GRE product manuafacture.

- Testing and Inspection Requirements.

- All GRP/GRE pipes and fittings shall undergo visual inspection to verify that they are free from defects such as cracks, blisters, voids, delamination, or fiber exposure.

- Dimensional inspection shall be conducted to confirm diameter, wall thickness, and length comply with the specified tolerances.

- Bonded or laminated joints shall be inspected to ensure proper curing and bonding quality.

- The installed piping system shall be subjected to hydrostatic pressure testing in accordance with the applicable project specification and standards.

- Pressure testing shall be conducted after sufficient curing time of adhesive joints as recommended by the manufacturer.

- Any defects identified during inspection or testing shall be repaired or replaced in accordance with approved repair procedures.

- All inspection and testing activities shall be documented in accordance with the Inspection and Test Plan (ITP).

- Inspection and testing shall include:

- Visual inspection of pipes and fittings

- Dimensional inspection

- Joint inspection after bonding

- Hydrostatic pressure testing

- Leak testing where required

All inspection and testing activities shall be documented.

- Installation Requirements.

- Installation of GRP/GRE piping shall follow the approved installation procedures and manufacturer’s installation manual.

- Pipes shall be handled carefully during transportation and installation to prevent impact damage, excessive bending, or surface damage.

- Piping shall be installed in accordance with the approved piping layout drawings, ensuring proper alignment and elevation.

- Proper pipe supports, guides, and anchors shall be installed to avoid excessive stress on the piping system.

- Jointing methods such as adhesive bonded joints, laminated joints, mechanical couplings, or flanged connections shall be performed by trained personnel.

- Flanged joints shall be assembled using approved gaskets and proper bolt tightening sequence to ensure uniform load distribution.

- Adequate curing time shall be allowed for bonded joints before pressure testing or commissioning.

- After installation and testing, the subcontractor shall submit inspection records, test reports, and as-built documentation for project completion and handover.

- Documentation Requirements.

The Contractor shall submit the following documents:

- Method Statement.

- Inspection and Test Plan (ITP).

- Material certificates.

- Fabrication records.

- Installation reports.

- Test reports.

- As-built drawings.

## Quality Assurancce and Quatily Control Requirements.

- The contractor shall establish a QA/QC program in compliance with ISO 9001-2015 quality management System.

- All Laminator / Bonder shall be trained, qualified and documented per ISO 14692

- The subcontractor shall prepare and submit Inspection and test plans (ITPs).

## Health, Safety and Environment (HSSE)

All activities shall comply with project HSSE requirements, including:

- Proper handling of resin and chemicals.

- Use of PPE during cutting and bonding.

- Safe lifting and rigging of piping line.

- Waste management and environmental protection.

# ATTACHMENT

###### Attachment #1: Isometric drawing and P&ID drawing.

###### Attachment #2: Material specification

###### Attachment #3: STG3 Line list